| TABLE 4. DETECTION LIMITS FOR THE INDUCTIVELY COUPLED PLASMA MASS SPECTROMETRY AND X-RAY FLUORESCENCE METHODS |
| --- |
| Method Code | Description | Elements and Ranges (%) |
| ME-XRF06 | Whole-rock analysis. All elements by lithium meta or tetra borate fusion and X-ray fluorescence | Si SiO2 (0.01–100) Al Al2O3 (0.01–100) Fe Fe2O3 (0.01–100) Ca CaO (0.01–100) Mg MgO (0.01–100) Na Na2O (0.01–100) K K2O (0.01–100) Cr Cr2O3 (0.01–100) Ti TiO2 (0.01–100) Mn MnO (0.01–100) P P2O5 (0.01–100) Sr SrO (0.01–100) Ba BaO (0.01–100) Loss on Ignition (0.01–100) |
|  |  | (ppm) |
| ME-MS61 | 47 elements | Ag (0.02–100) Al (0.01%–25%) As (0.2–10,000) Ba (0.5–10,000) Be (0.05–1000) Bi (0.01–10,000) Ca (0.01%–25%) Cd (0.02–500) Ce (0.01–500) Co (0.1–10,000) Cr (1–10,000) Cs (0.05–500) Cu (0.2–10,000) Fe (0.01%–25%) Ga (0.05–500) Ge (0.05–500) Hf (0.1–500) In (0.005–500) K (0.01%–10%) La (0.5–500) Li (0.2–500) Mg (0.01%–15%) Mn (5–10,000) Mo (0.05–10,000) Na (0.01%–10%) Nb (0.1–500) Ni (0.2–10,000) P (10–10,000) Pb (0.5–10,000) Rb (0.1–500) Re (0.002–50) S (0.01%–10%) Sb (0.05–1000) Se (1–1000) Sn (0.2–500) Sr (0.2–10,000) Ta (0.05–100) Te (0.05–500) Th (0.2–500) Ti (0.01%–10%) Tl (0.02–500) U (0.1–500) V (1–10,000) W (0.1–10,000) Y (0.1–500) Zn (2–10,000) Zr (0.5–500) |

[[AU: should values in %, e.g., (0.01%–25%), be separate from ppm values?]]